## Slide 1
Residual stress measurement of additive manufactured support-less metal parts

## Slide 2: Challenges and Impact
Challenges
  To reduce the dross and wrap.
  Accumulation of residual stress.
Impact
  Distort the dimensional accuracy of part, which may damage recoter.
  Forming failure of part surfaces.
Warp
Dross

## Slide 3
Design Sample
Support recommended by Magics
Actual Support

## Slide 4
XRD Analysis :-
Nanoindentation Analysis :-
Radiation | Wavelength | Current | Tension | Psi (Ψ) | Phi (ø) | Lattice Parameter [hkl]
Co Kα | 1.79Å | 30 mA | 40 KV | -45 to 45 | 90 | 211
Indenter | Acquisition Rate | Maximum Load | Loading Time | Holding Time | Unloading Time | Approach Speed | Retract Speed
Spherical Diamond | 10 Hz | 200 mN | 30 sec | 10 sec | 30 sec | 2000 mm/min | 2000 mm/min

## Slide 5
X-Ray Diffraction Analysis
Effect of Height
Height (mm) | 1.6 | 3.2 | 4.8
Normal Stress (Mpa) | 206±76.9 | 230.6±57.3 | 248.9±62

## Slide 6
Angle | 25 | 35 | 45
Normal Stress (Mpa) | 360±13.8 | 265±60 | 248.9±62
Effect of Overhang Angle

## Slide 7
Fabrication and Characterization of Different Supportless Overhang Structures Using DMLS
04 May 2017
Width (mm) | 2.5 | 3.5 | 5
Normal Stress (Mpa) | 221.3±28.3 | 315±65.4 | 248.9±62
Effect of Width

## Slide 8
Nano Indentation Analysis
Effect of Height
Height (mm) | 1.6 | 3.2 | 4.8
Indentation (nm) | 1366.80 | 1376.20 | 1392.35
Angle | 25 | 35 | 45
Indentation (nm) | 1418.31 | 1414.59 | 1392.35
Width (mm) | 2.5 | 3.5 | 5
Indentation (nm) | 1379.07 | 1447.22 | 1392.35
Effect of Overhang Angle
Effect of Width

## Slide 9
For Stress Free Sample:-
Average indentation depth obtain for the stress free sample is 1074.42nm

## Slide 10
04 May 2017
•We successful built the overhang angle below the critical angle, although the surface quality is poor.
•The value of residual stress increases with increase of height. Although it is not above the yield stress of used material but if we increase height more there us chance of crack generation is there.
•Residual stress also increases as we lower the overhang angle, so for small angle the height of sample needs to be small.
•For the scan length (width), residual stress is also depend on the rate of cooling.
•The result of nanoindentation also matches with the result proﬁle of XRD method.
Conclusion

## Slide 11: Conference Paper
Study on the Effect of Different Process Parameters on the Quality of Overhang Surface Produced by Direct Metal Laser Sintering Process by Sagar Sarkar, Ankit Porwal, Cheruvu Siva Kumar and Ashish Kumar Nath, Proceedings of National Conference on Advanced Functional Materials Processing Manufacturing (NCAFMPM-2017), Excel India Publishers ,New Delhi, 96-100 (2017).